## Slide 1
The crystal Structures of Ionic Materials: Pauling groups, Crystal types: simple cubic (c), body centered cubic (bcc), face centered cubic (fcc/ccp) hexagonal close packed (hcp) etc., tetrahedral and octahedral holes, coordination number, unit cell, crystal systems, Miller indices and their significance.

## Slide 2
We can assume minerals to be made of orderly packing of atoms or rather ions or molecules.
Many mineral properties like symmetry, density etc are dependent on how the atoms or ions are packed
We can approximate the atoms or ions in a metal to be rigid spherical balls

## Slide 3
Think of a box full of ping pong balls.
The densest packing is one on which a layer of balls sit on the hollow between the balls in the layer below.
The two closest packing are:
Hexagonal close packing (ABCABC)
Cubic close packing (ABAB)

## Slide 4
Closest packing of spheres.

## Slide 5
Some what less dense packing is body centered cubic packing, seen in Iron.
Because they can be packed so closely, metals have high density

## Slide 6
Body-centered cubic packing.
(a) Bodycentered lattice (left) and with atoms at each lattice node (right).
(b) Eight unit cells.
Each sphere is in contact with eight neighbors.

## Slide 7: Covalent and Molecular Bonds
Covalent bonds are strong therefore covalent crystals are strong and have high melting point
Because atoms need to be placed in a specific orientation only, covalent crystals do not show a close packing.
The bonds in molecular crystals are weak, hence these tend to be soft.
The geometry of the structure is determined by the shape and charge distribution in the molecules (e.g., Hydrogen bond in water)

## Slide 8: Ionic Bonds
For minerals formed largely by ionic bonding, the ion geometry can be simply considered to be spherical
Spherical ions will geometrically pack (coordinate) oppositely charged ions around them as tightly as possible while maintaining charge neutrality
For a particular ion, the surrounding coordination ions define the apices of a polyhedron
The number of surrounding ions is the Coordination Number

## Slide 9: Pauling’s Rules of Mineral Structure
Rule 1:
A coordination polyhedron of anions is formed around each cation, wherein:
- the cation-anion distance is determined by the sum of the ionic radii, and
- the coordination number of the polyhedron is determined by the cation/anion radius ratio (Rc:Rx)

## Slide 10
Radius Ratio of Cation and Anion (Rc/Ra), Coordination number and Coordination polyhedra

## Slide 11
Minimum Radius Ratio | Coordination number | Packing geometry
~1.0 | 12 | Corners of a cuboctahedron (close packing)
0.732-1 | 8 | Corners of a cube
0.414- 0.732 | 6 | Corners of a octahedron
0.225- 0.414 | 4 | Corners of a tetrahedron
0.155- 0.225 | 3 | Corners of an equilateral triangle
<0.155 | 2 | Linear

## Slide 13
Rule 2: The electrostatic valency principle
The strength of an ionic (electrostatic) bond (e.v.) between a cation and an anion is equal to the charge of the anion (z) divided by its coordination number (n):
e.v. = z/n
In a stable (neutral) structure, a charge balance results between the cation and its polyhedral anions with which it is bonded.

## Slide 14: Charge Balance of Ionic Bonds

## Slide 15: Uniform Bond Strength
Isodesmic: where all ionic bonds are of equal strength
Anions tend to pack around the cation in highly symmetric and generally close packing arrangement
Most of the minerals crystallize in highly symmetric systems like isometric, tetragonal or hexagonal systems
Oxides, Fluorides, Chlorides are common examples

## Slide 17: Nonuniform Bond Strength
Some anion-cation bonds are stronger than others: cations forming stronger bonds are smaller and have a high charge
– Eg: C4+, S6+, P5+, Si4+
– These strongly charged cations from CO32-, SO44-, PO43-,SiO44- anionic groups
Have lower symmetry, irregular coordination polyhedra

## Slide 18: Formation of Anionic Groups
Anisodesmic Bonds results from high valence cations with electrostatic valencies greater than half the valency of the polyhedral anions; other bonds with those anions will be relatively weaker.
Mesodesmic: anion-cation bond takes exactly half othe available anioncation charge

## Slide 19: Anisodesmic

## Slide 21
Anisodesmic carbonate (CO32−) group. Each O–C bond occupies 1.33 of the available –2 charge on oxygen; only two-thirds of a charge on the oxygen is available to bond with other cations such as Ca2+.

## Slide 22
Mesodesmic silicon tetrahedra.

## Slide 23
Rule 3: Anion polyhedra that share edges or faces decrease their stability due to bringing cations closer together; especially significant for high valency cations

## Slide 24
Rule 4: In structures with different types of cations, those cations with high valency and small CN tend not to share polyhedra with each other; when they do, polyhedra are deformed to accommodate cation repulsion

## Slide 25
Sharing anions between polyhedra.

## Slide 26
Rule 5: The principle of parsimony : nature tends towards simplicity
Because the number and types of different structural sites tends to be limited, even in complex minerals, different ionic elements are forced to occupy the same structural positions – leads to solid solution.

## Slide 27
NaCl structure.

## Slide 28
Anhydrite structure. Isolated SO42− groups are bonded laterally through Ca2+ (dark spheres).

## Slide 29
Crystal types: simple cubic (c), body centered cubic (bcc), face centered cubic (fcc/ccp) hexagonal close packed (hcp) etc.,

## Slide 30
Type
Ionic
Covalent
Metallic
Secondary
Bond Energy
Large!
Variable
large-Diamond
small-Bismuth
Variable
large-Tungsten
small-Mercury
smallest
Comments
Nondirectional (ceramics)
Directional
semiconductors, ceramics
polymer chains)
Nondirectional (metals)
Directional
inter-chain (polymer)
inter-molecular
SUMMARY: BONDING

## Slide 31
• Bond length, r
• Bond energy, Eo
• Melting Temperature, Tm
Tm is larger if Eo is larger.
PROPERTIES FROM BONDING: TM

## Slide 32
• Elastic modulus, E
• E ~ curvature at ro
E is larger if Eo is larger.
PROPERTIES FROM BONDING: E
• E ~ curvature at ro

## Slide 33
• Coefficient of thermal expansion, a
• a ~ symmetry at ro
a is larger if Eo is smaller.
PROPERTIES FROM BONDING: a

## Slide 34
Ceramics
(Ionic & covalent bonding):
Metals
(Metallic bonding):
Polymers
(Covalent & Secondary):
Large bond energy
large Tm
large E
small a
Variable bond energy
moderate Tm
moderate E
moderate a
Directional Properties
Secondary bonding dominates
small T
small E
large a
SUMMARY: PRIMARY BONDS

## Slide 35: CHAPTER 3: Structures of Metals and Ceramics
ISSUES TO ADDRESS...
• How do atoms assemble into solid structures?
• How does the density of a material depend on
its structure?
• When do material properties vary with the
sample (i.e., part) orientation?
1
How do the structures of ceramic materials differ from those of metals?

## Slide 36: ENERGY AND PACKING
2
• Non dense, random packing
• Dense, regular packing
Dense, regular-packed structures tend to have
lower energy.

## Slide 38: Lattice and Unit Cells
Lattices:
The simplest regular array is a line of evenly spaced objects.
There is a dot at the same place in each objects.
a

## Slide 39
The line of the dots is called the lattice and each lattice point must have identical surroundings.

## Slide 40: One and Two dimensional Unit Cell
The unit cell for the 1-D lattice lies between two vertical lines.
a

## Slide 41
The unit or the 2-D lattices are parallelograms with their corners at equivalent positions in the array.
5
1
2
3
4

## Slide 42
Five 2-D lattices are possible.

## Slide 43: Three dimensional unit cell
The unit cell of a 3-D is defined by three distance a,b and c and three angles ,  and .
x
y
z




## Slide 44
Since the unit cells are the basic building blocks of the crystals, they must be space filling.
The 3-D unit cell includes four different types.
1. The primitive cell – has a lattice point at each corner.
2. The body centered unit cell- has a lattice point at each corner and one at the center of the cell.
3. The face centered unit cell – has a lattice point at each corner and one in the center of each face.
4. The face centered unit cell – has a lattice point at each corner and one in the centers of one pair of opposite faces. (eg., an A centered cell has lattice point in the centeres of the bc faces)

## Slide 45
These are known as the seven crystal systems or classes.

## Slide 46
14 different point lattices, called Bravais lattices, make up the crystal system. The lengths of the sides, a, b, and c, and the angles between them can vary for a particular unit cell.

## Slide 48: METALLIC CRYSTALS
3
• tend to be densely packed.
• have several reasons for dense packing:
-Typically, only one element is present, so all atomic
radii are the same.
-Metallic bonding is not directional.
-Nearest neighbor distances tend to be small in
order to lower bond energy.
• have the simplest crystal structures. 74 elements
have the simplest crystal structures – BCC, FCC and HCP
We will look at three such structures...

## Slide 50
The crystal lattice
A point lattice is made up of regular, repeating points in space. An atom or group of atoms are tied to each lattice point

## Slide 51
14 different point lattices, called Bravais lattices, make up the crystal system. The lengths of the sides, a, b, and c, and the angles between them can vary for a particular unit cell.

## Slide 52: Three simple lattices that describe metals are Face Centered Cubic (FCC) Body Centered Cubic (BCC) and Hexagonal Close Packed (HCP)

## Slide 53: SIMPLE CUBIC STRUCTURE (SC)
4
• Rare due to poor packing (only Po has this structure)
• Close-packed directions are cube edges.
• Coordination # = 6
(# nearest neighbors)
(Courtesy P.M. Anderson)
Click on image to animate

## Slide 54: ATOMIC PACKING FACTOR
5
• APF for a simple cubic structure = 0.52
Adapted from Fig. 3.19,
Callister 6e.

## Slide 55: FACE CENTERED CUBIC STRUCTURE (FCC)
6
• Coordination # = 12
Adapted from Fig. 3.1(a),
Callister 6e.
(Courtesy P.M. Anderson)
• Close packed directions are face diagonals.
--Note: All atoms are identical; the face-centered atoms are shaded
differently only for ease of viewing.
Click on image to animate

## Slide 56: ATOMIC PACKING FACTOR: FCC
7
• APF for a body-centered cubic structure = 0.74
Adapted from
Fig. 3.1(a),
Callister 6e.

## Slide 57: BODY CENTERED CUBIC STRUCTURE (BCC)
• Coordination # = 8
8
Adapted from Fig. 3.2,
Callister 6e.
(Courtesy P.M. Anderson)
• Close packed directions are cube diagonals.
--Note: All atoms are identical; the center atom is shaded
differently only for ease of viewing.
Click on image to animate

## Slide 58: ATOMIC PACKING FACTOR: BCC
9
• APF for a body-centered cubic structure = 0.68
Adapted from
Fig. 3.2,
Callister 6e.

## Slide 59: HEXAGONAL CLOSE-PACKED STRUCTURE (HCP)
10
• Coordination # = 12
• ABAB... Stacking Sequence
• APF = 0.74
• 3D Projection
• 2D Projection
Adapted from Fig. 3.3,
Callister 6e.

## Slide 60: THEORETICAL DENSITY, r
11
Example: Copper
Data from Table inside front cover of Callister (see next slide):
• crystal structure = FCC: 4 atoms/unit cell
• atomic weight = 63.55 g/mol (1 amu = 1 g/mol)
• atomic radius R = 0.128 nm (1 nm = 10 cm)
-7

## Slide 61: Characteristics of Selected Elements at 20C
12
Adapted from
Table, "Charac-
teristics of
Selected
Elements",
inside front
cover,
Callister 6e.

## Slide 62: DENSITIES OF MATERIAL CLASSES
13
Why?
Metals have...
• close-packing
(metallic bonding)
• large atomic mass
Ceramics have...
• less dense packing
(covalent bonding)
• often lighter elements
Polymers have...
• poor packing
(often amorphous)
• lighter elements (C,H,O)
Composites have...
• intermediate values
Data from Table B1, Callister 6e.

## Slide 63: CERAMIC BONDING
14
• Bonding:
--Mostly ionic, some covalent.
--% ionic character increases with difference in
electronegativity.
Adapted from Fig. 2.7, Callister 6e. (Fig. 2.7 is adapted from Linus Pauling, The Nature of the Chemical Bond, 3rd edition, Copyright 1939 and 1940, 3rd edition. Copyright 1960 by
Cornell University.
• Large vs small ionic bond character:

## Slide 64: IONIC BONDING & STRUCTURE
15
• Charge Neutrality:
--Net charge in the
structure should
be zero.
--General form:
• Stable structures:
--maximize the # of nearest oppositely charged neighbors.
Adapted from Fig. 12.1, Callister 6e.

## Slide 65: COORDINATION # AND IONIC RADII
16
• Coordination # increases with
Issue: How many anions can you
arrange around a cation?
Adapted from Table 12.2, Callister 6e.
Adapted from Fig. 12.2, Callister 6e.
Adapted from Fig. 12.3, Callister 6e.
Adapted from Fig. 12.4, Callister 6e.

## Slide 66: EX: PREDICTING STRUCTURE OF FeO
17
• On the basis of ionic radii, what crystal structure
would you predict for FeO?
• Answer:
based on this ratio,
--coord # = 6
--structure = NaCl
Data from Table 12.3, Callister 6e.

## Slide 67: AmXp STRUCTURES
18
• Consider CaF2 :
• Based on this ratio, coord # = 8 and structure = CsCl.
• Result: CsCl structure w/only half the cation sites
occupied.
• Only half the cation sites
are occupied since
#Ca2+ ions = 1/2 # F- ions.
Adapted from Fig. 12.5, Callister 6e.

## Slide 68: DEMO: HEATING AND COOLING OF AN IRON WIRE
19
• Demonstrates "polymorphism"
The same atoms can have more than one crystal structure.

## Slide 69: FCC STACKING SEQUENCE
20
• ABCABC... Stacking Sequence
• 2D Projection
• FCC Unit Cell

## Slide 70: STRUCTURE OF COMPOUNDS: NaCl
21
• Compounds: Often have similar close-packed structures.
• Close-packed directions
--along cube edges.
• Structure of NaCl
(Courtesy P.M. Anderson)
(Courtesy P.M. Anderson)
Click on image to animate
Click on image to animate

## Slide 71: Diamond, BeO and GaAs are examples of FCC structures with two atoms per lattice point

## Slide 72: CRYSTALS AS BUILDING BLOCKS
22
• Some engineering applications require single crystals:
• Crystal properties reveal features
of atomic structure.
(Courtesy P.M. Anderson)
--Ex: Certain crystal planes in quartz
fracture more easily than others.
--diamond single
crystals for abrasives
--turbine blades
Fig. 8.30(c), Callister 6e.
(Fig. 8.30(c) courtesy
of Pratt and Whitney).
(Courtesy Martin Deakins,
GE Superabrasives, Worthington, OH. Used with permission.)

## Slide 73: POLYCRYSTALS
23
• Most engineering materials are polycrystals.
• Nb-Hf-W plate with an electron beam weld.
• Each "grain" is a single crystal.
• If crystals are randomly oriented,
overall component properties are not directional.
• Crystal sizes typ. range from 1 nm to 2 cm
(i.e., from a few to millions of atomic layers).
Adapted from Fig. K, color inset pages of Callister 6e.
(Fig. K is courtesy of Paul E. Danielson, Teledyne Wah Chang Albany)
1 mm

## Slide 74: SINGLE VS POLYCRYSTALS
24
• Single Crystals
-Properties vary with
direction: anisotropic.
-Example: the modulus
of elasticity (E) in BCC iron:
• Polycrystals
-Properties may/may not
vary with direction.
-If grains are randomly
oriented: isotropic.
(Epoly iron = 210 GPa)
-If grains are textured,
anisotropic.
200 mm
Data from Table 3.3, Callister 6e.
(Source of data is R.W. Hertzberg, Deformation and Fracture Mechanics of Engineering Materials, 3rd ed., John Wiley and Sons, 1989.)
Adapted from Fig. 4.12(b), Callister 6e.
(Fig. 4.12(b) is courtesy of L.C. Smith and C. Brady, the National Bureau of Standards, Washington, DC [now the National Institute of Standards and Technology, Gaithersburg, MD].)

## Slide 75: MATERIALS AND PACKING
• atoms pack in periodic, 3D arrays
• typical of:
26
Crystalline materials...
-metals
-many ceramics
-some polymers
• atoms have no periodic packing
• occurs for:
Noncrystalline materials...
-complex structures
-rapid cooling
crystalline SiO2
noncrystalline SiO2
"Amorphous" = Noncrystalline
Adapted from Fig. 3.18(b),
Callister 6e.
Adapted from Fig. 3.18(a),
Callister 6e.

## Slide 76: GLASS STRUCTURE
28
• Quartz is crystalline
SiO2:
• Basic Unit:
• Glass is amorphous
• Amorphous structure
occurs by adding impurities
(Na+,Mg2+,Ca2+, Al3+)
• Impurities:
interfere with formation of
crystalline structure.
(soda glass)
Adapted from Fig. 12.11, Callister, 6e.

## Slide 77: SUMMARY
• Atoms may assemble into crystalline or
amorphous structures.
• We can predict the density of a material,
provided we know the atomic weight, atomic
radius, and crystal geometry (e.g., FCC,
BCC, HCP).
• Material properties generally vary with single
crystal orientation (i.e., they are anisotropic),
but properties are generally non-directional
(i.e., they are isotropic) in polycrystals with
randomly oriented grains.
27

## Slide 78: Miller Indices
The faces of the crystals both when they grow and when they are formed by cleavage
Tent to be parallel either to the sides of the unit cell or to planes in the crystals.
It is useful to be able to refer to both crystal faces and to the planes  by Miller indices.